Sezione di Genova

Sezione di Milano

Laboratori Nazionali di Frascati

INFN/code-09/001

12 Novembre 2008

TECHNICAL DESIGN REPORT 
OF A SUPERCONDUCTING MODEL DIPOLE FOR FAIR SIS300

F.Alessandria2, S.Angius4, G.Bellomo2, P.Fabbricatore1, S.Farinon1, U.Gambardella3, R.Marabotto4, R.Musenich1, R.Repetto4, M.Sorbi2 and G.Volpini2

1)INFN-Sezione di Genova, Via Dodecaneso 33, 16146 Genova, Italy

2)INFN-Sezione di Milano, Laboratorio LASA, Via Fratelli Cervi 201, 
20090 Segrate (MI), Italy

3)INFN-Laboratori Nazionali di Frascati Via E. Fermi 40, I-00044 Frascati, Italy

4)ASG-Superconductors, Corso Perrone 73R, Genova, Italy

Abstract

This report deals with the R&D activities aimed at developing the high field rapidly-cycling super-conducting dipoles needed for SIS300 synchrotron of the FAIR facility at GSI. The present lattice design includes 48 long dipoles with magnetic length 7.757 m and 12 short dipoles with magnetic length 3.879 m. The coils have two main features: they are curved (the corresponding sagitta is 112.8 mm for long dipoles), and they are fast ramped (for a superconducting magnet). Both these characteristics demand a challenging R&D, aimed at the development of the required low loss conductor, a robust design with respect to fatigue issues and a suitable winding technology. The Italian National Institute of Nuclear Physics (INFN) is performing this R&D. A project, called DISCORAP (“Dipoli SuperCOnduttori RApidamente Pulsati”), started in 2006 in accordance with a specific INFN-FAIR Memorandum of Understanding signed by both institutions in December 2006. The aim is to have a complete cold mass model of the short dipole ready in the summer of 2009. After a preliminary test of the cold mass in a vertical cryostat, it will be integrated into a horizontal cryostat for a test series at GSI.

Published by SIS–Pubblicazioni

Laboratori Nazionali di Frascati