## GSI Fast-Pulsed Synchrotron Magnet Project: MNW Report GSI 2 version 2

## Martin Wilson 31 Dec 00

AC Losses for Different Cycles in RHIC Dipole Magnets

###### Preface

An error has been found in the field components which are the basis of all ac loss calculations in Reports 1 to 4.  The error occurred in converting from Cartesian to polar  components of field and had the effect of increasing the transverse or ‘’ component of field, particularly near to the poles, thereby increasing the total loss by about a factor 2.  Please destroy Report 2-1

##### Introduction

This report uses the algorithms presented in Report 1 to calculate the losses in a 3m long RHIC dipole magnet, made from three different types of cable, when ramped with three different cycles.  Because the defined cycles contain significant pauses for injection and extraction, in some cases the time averaged loss is reduced significantly below the loss during ramping.

##### The Synchrotron Cycles

With the nomenclature defined in Fig 1, Table 1 presents the three cycles calculated here.  They are the cycles presented by G Moritz during the meeting of 19 Sept at Virginia Beach.

Fig 1: Nomenclature for the synchrotron cycles

Table 1: Parameters for the synchrotron cycles

| cycle | f | Bi | Be | B` | Ti | Te | Tr | Tc | 1/Tc |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | =Bi / Be | T | T | T/s | s | s | s | s | Hz |
| 1 | 0.2 | 0.2 | 1 | 4 | 0 | 0 | 0.2 | 0.4 | 2.5 |
| 2 | 0.1 | 0.2 | 2 | 4 | 1.5 | 0 | 0.45 | 2.4 | 0.4167 |
| 3 | 0.05 | 0.175 | 3.5 | 1.75 | 1.5 | 1 | 1.9 | 6.3 | 0.1587 |

##### The Cables

The cables used are exactly the same as those defined in Report 1, with the parameters listed in Table 2.

Table 2: Key parameters of cables used in the ac loss calculations

| parameter |  | symbol | RHIC | core 1 | core 2 | unit |
| --- | --- | --- | --- | --- | --- | --- |
| cable half width |  | a | 4.87E-03 | 4.87E-03 | 4.87E-03 | m |
| cable half thickness |  | b | 5.83E-04 | 5.83E-04 | 5.83E-04 | m |
| cable twist pitch |  | p | 7.40E-02 | 7.40E-02 | 7.40E-02 | m |
| crossover resistance |  | Rc | 5.00E-05 | 1.00E-03 | 4.00E-03 | m |
| adjacent resistance |  | Ra | 3.50E-04 | 2.00E-05 | 9.00E-05 | W |
| number of strands |  | N | 30 | 30 | 30 |  |
| crossover resistance. area |  | rc | 4.00E-11 | 8.00E-10 | 3.20E-09 | m2 |
| adjacent resistance. area |  | ra | 2.80E-10 | 1.60E-11 | 7.20E-11 | m2 |
| effective longitudinal resistivity |  | x | 2.89E-08 | 1.65E-09 | 7.42E-09 | m |
| cable filling factor |  | c | 0.826 | 0.826 | 0.826 |  |
| wire filling factor |  | w | 0.872 | 0.872 | 0.872 |  |
| filament filling factor |  | f | 0.308 | 0.308 | 0.308 |  |
| wire transverse resistivity |  | t | 5.67E-10 | 5.67E-10 | 5.67E-10 | m |
| wire twist pitch |  | pw | 1.33E-02 | 6.00E-03 | 4.00E-03 | m |
| wire coupling time const |  |  | 4.99E-03 | 1.01E-03 | 4.49E-04 | s |
| filament diameter |  | df | 6.00E-06 | 6.00E-06 | 6.00E-06 | m |

##### The calculated losses

Details of the calculations are presented in Appendices 1 – 3, corresponding to cycles 1 – 3.  Note that, throughout the body of the spreadsheets, losses are calculated as an average loss over the ramping times; finally, the ‘time averaged’ loss is calculated as a lower value which includes the ‘dead time’ for injection and extraction.  Results from the Appendices are summarised in Table 3

Table 3: Results of the loss calculations

| cycle # | cable type  | RHIC | core 1 | core2 |
| --- | --- | --- | --- | --- |
| 1 | ramping total loss / magnet = | 956 W | 171 W | 93 W |
| 1 | time averaged total loss / magnet = | 956 W | 171 W | 93 W |
| 1 | transverse crossover loss / total = | 71.8% | 20.0% | 9.2% |
| 1 | transverse adjacent loss / total = | 0.21% | 20.7% | 8.5% |
| 1 | parallel loss / total = | 0.01% | 0.69% | 0.28% |
| 1 | filament coupling loss / total = | 22.0% | 25.0% | 20.4% |
| 1 | hysteresis loss / total = | 6.0% | 33.6% | 61.6% |
| 2 | ramping total loss / magnet = | 943 W | 157 W | 79 W |
| 2 | time averaged total loss / magnet = | 353 W | 59 W | 30 W |
| 2 | transverse crossover loss / total = | 72.8% | 21.8% | 10.8% |
| 2 | transverse adjacent loss / total = | 0.21% | 22.5% | 9.9% |
| 2 | parallel loss / total = | 0.01% | 0.75% | 0.33% |
| 2 | filament coupling loss / total = | 22.3% | 27.1% | 23.9% |
| 2 | hysteresis loss / total = | 4.6% | 27.7% | 55.0% |
| 3 | ramping total loss / magnet = | 187 W | 37 W | 22 W |
| 3 | time averaged total loss / magnet = | 113 W | 22 W | 13 W |
| 3 | transverse crossover loss / total = | 70.1% | 17.8% | 7.5% |
| 3 | transverse adjacent loss / total = | 0.21% | 18.4% | 6.8% |
| 3 | parallel loss / total = | 0.01% | 0.61% | 0.23% |
| 3 | filament coupling loss / total = | 21.5% | 22.1% | 16.5% |
| 3 | hysteresis loss / total = | 8.1% | 41.2% | 69.0% |

##### Conclusions

Cycles 1 and 2 show similar ramping losses to those calculated in Report 1, because the loss is dominated by B`.  However, when the dead time for injection is included, the time averaged loss for Cycle 2 is greatly reduced.   The lower ramp rate of Cycle 3 gives ramping losses ~ ¼ of Report 1, with time averaged loss being even smaller.