GSI Fast-Pulsed Synchrotron Project:

MNW Report GSI 20 version 1

22 Jul 04

Calculation of Loss in the SIS300 Dipole

1.  Introduction

This Report uses field shape data from Carsten Muehle to set up a new loss calculating spreadsheet for the SIS300 dipole.  It then calculates losses for a range of assumptions about cable parameters and compares the results with an existing calculation by IHEP.

2. Loss Calculation Method

Appendix 20-1(1) reproduces the field shape data provided by Carsten Muehle [1].  The sheets 'Brad' and 'Bphi' sort the data into plots in a radial direction at 1 degree intervals.  As described in my Report 1, this data is then fitted along each degree line by a constant Brad  and a B which varies linearly across the cable width.  Thus at each degree point we a have values for Bparallel  (= Brad)  Btrans (=B at cable centre) and Gtrans  (=gradient of B).  These values are then copied into Appendix 20-4(1) where they are used to calculate losses: note the approximation that 'radial' is parallel to the cable, may not always be exact.

With the correct definition of et [2], it is necessary to define a boundary radius for the filament bundle.  Appendix 20-2(1) calculates this radius for some reasonable assumptions about copper wall thicknesses, but note that this is only an estimate and the feasibility of making a double stack wire with such a low matrix:superconductor ratio and good filament shape has yet to be confirmed.

Appendix 20-3(1) calculates cable size and filling factors and compares them with LHC and RHIC cables.  It also estimates the inter-strand resistances that would arise if the wire surface etc were the same as in Dipole001.

Appendix 20-4(1) calculates losses with the same assumptions that have evolved over my previous Reports, eg Rep 14 and 22.  The main changes are the different field shape and the presence of 2 layers in the coil, which means that the segment volumes for integration must be calculated separately for inner and outer coils.

Appendix 20-5(1) presents the formulae used in the calculation and checks the numbers for the 20 degree line of the inner coil.

3. Loss Calculation Input Data.

Most of the input data, I took from [3], but I also used the Jc(B) fit and et(B)  from [2].  Maximum field is 6T, injection field 1.6T and ramp rate 1T/s.  Table 1 lists the main parameters which remained constant throughout the cases.  I ran four cases and Table 2 lists the parameters which I changed between these cases.  As in previous Reports, the wire effective transverse resistivity is fitted by:

ρet(B)=Cet+metB	(1)

and the critical current density by the modified Kim Anderson formula

Jc=JoBoB+Bo+A0+A1B	(2)

For the transport current correction to hysteresis loss I use the simple Kim Anderson formula

(3)

Table 1: Parameters which remained constant throughout

| cable half width | c m | 7.64E-03 |
| --- | --- | --- |
| cable half thickness | b m | 8.44E-04 |
| cable twist pitch | p m | 1.00E-01 |
| number of strands | N | 36 |
| wire radius | aw mm | 0.4125 |
| radius of filament boundary | afb mm | 0.3713 |
| cable filling factor | c | 0.880 |
| wire filling factor | w | 0.847 |
| matrix ratio | mat | 1.400 |
| filament filling factor | f | 0.417 |
| filament diameter | df m | 3.5 |
| wire twist pitch | pw mm | 6.0 |
| max magnet current | Iext A | 5954 |
| max aperture field | Bext T | 6.00 |
| min magnet field | Binj T | 1.6 |
| min magnet current | Iinj A | 1588 |
| cooking factor transverse Rc | ftc | 1.00 |
| cooking factor transverse Ra | fta | 2.00 |
| cooking factor parallel Ra | fpa | 1.00 |
| cooking factor hysteresis | fh | 1.00 |

Table 2: Parameters which were changed through the 4 cases

| Case |  | 1 | 2 | 3 | 4 |
| --- | --- | --- | --- | --- | --- |
| crossover resistance | Rc  | 2.00E-02 | 2.00E-02 | 4.30E-02 | 2.00E-02 |
| adjacent resistance | Ra  | 1.00E-04 | 1.00E-04 | 3.88E-05 | 1.00E-04 |
| wire transverse resistivity intercept | Cret m | 1.00E-10 | 1.24E-10 | 1.24E-10 | 1.00E-10 |
| wire transverse resistivity gradient | mret mT-1 | 2.00E-11 | 9.00E-11 | 9.00E-11 | 2.00E-11 |
| Modified Kim Anderson | J0 Am-2 | 3.50E+10 | 3.50E+10 | 3.50E+10 | 1.62E+10 |
| Modified Kim Anderson | B0 T | 0.149 | 0.149 | 0.149 | 1.00 |
| Modified Kim Anderson | A0 | 5.00E+09 | 5.00E+09 | 5.00E+09 | 0.00E+00 |
| Modified Kim Anderson | A1 | -7.0E+08 | -7.0E+08 | -7.0E+08 | 0.0E+00 |
| Kim Anderson | Jso Am-2 | 3.20E+10 | 3.20E+10 | 3.20E+10 | 1.62E+10 |
| Kim Anderson | Bso T | 0.5 | 0.5 | 0.5 | 1.00 |

4. Loss Calculation Results.

Table 3 summarizes my results, with the final column reproducing the IHEP results reported in [4].  With the specified [3]  et(B), it may be seen that filament coupling via the matrix dominates.  Using the et(B) measured for RHIC wire  in case 2 reduces this loss appreciably, and I can see no good reason for using the lower resistivity.  Case 2 is my best estimate of the loss at present.

Table 3: Summary of Loss Results

|  | loss per cycle per metre of magnet (Joules) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 1) spec | 2) RHIC | 3) dip001 | 4) IHEP | 5) IHEP [4] |
| transverse field via Rc | 3.2 | 3.2 | 1.5 | 3.2 | 8.9 |
| transverse field via Ra | 21.3 | 21.3 | 54.9 | 21.3 | 15.6 |
| parallel field via Ra | 0.2 | 0.2 | 0.5 | 0.2 | 0.2 |
| filament coupling via et | 89.7 | 39.2 | 39.2 | 89.7 | 122.9 |
| hysteresis loss | 46.9 | 46.9 | 46.9 | 42.6 | 42.3 |
| transport current correction to hysteresis | 1.0 | 1.0 | 1.0 | 1.1 | 0 |
| total hysteresis | 47.9 | 47.9 | 47.9 | 43.7 | 42.3 |
| total magnet loss | 162.4 | 111.9 | 144.2 | 158.2 | 189.9 |

In case 3, I use the values of Rc and Ra obtained in Appendix 20-3(1) by scaling the Dipole 001 numbers, ie this is what we expect to get if we do nothing different.  The transverse field coupling via Ra now dominates, so there will clearly be some benefit in trying to increase Ra, eg by the CERN heat treatment.

In case 4 I try to reproduce the IHEP calculation using the numbers given in [4].  The only difference from case 1) is that, for hysteresis loss, I use a simple Kim Anderson model of Jc(B) with Jo adjusted to get the specified Jc  of 2700Amm-2  at 5T and do not apply a transport current correction.  Column 5) reproduces the IHEP results in [4].  It may be seen that we agree well on hysteresis and parallel field losses, but less well on the rest.  For filament coupling via et the difference may be because I now calculate loss within the filament boundary radius [Rep 19(2)].  For the transverse field I have applied the cooking factor of 2, which roughly estimates the measured effect of Ra being lower at the cable edges.  Without the factor 2, I am calculating lower than IHEP, also for the transverse field loss via Rc.  I have no explanation for these discrepancies, we need to chase them.

5. Conclusions

a) Case 2 is my best estimate of SIS300 loss

b) IHEP and I agree on hysteresis loss, and my corrections and more complicated  Jc(B) model don't make much difference

c) We should definitely increase the Ra of Staybrite via the CERN heat treatment, or think about a different coating.

d) The specified et(B) gives much high inter-filament coupling loss than the measured values.   However, going to the low matrix:superconductor of  1.4:1 means that the inter-filament spacing will be lower in SIS300, so et(B) is also likely to be lower.  Perhaps this lower et(B) with copper should encourage us to use CuMn.

e) IHEP and I disagree on cable losses in both perpendicular and parallel field - we need to sort this out, perhaps by calculating a very simple magnet, eg uniform field.

Appendices

Appendix 20-1(1): SIS300 field shape

Appendix 20-2(1): Internal dimensions of the wire

Appendix 20-3(1): SIS300 Cable Parameters

Appendix 20-4(1): Hysteresis and coupling losses in SIS300

Appendix 20-5(1): Formulae used in magnet loss calculation, plus numerical check

References

[1]  Carsten Muehle email 5 Apr 04 'SIS300 data'.

[2] 	MNW Report 19(2), arising from email by Arup Ghosh

[3] 	Juris Kaugerts ' Proposed SIS 300 6 T Dipole Conductor Parameters', circulated by email 4 June 04

[4] 	Final Report on the Research and Development Contract Design of 6T Superconducting Dipoles for the SIS300, June 04 Chapter 29 Appendix 3