GSI Fast-Pulsed Synchrotron Project:

MNW Report GSI 21 version 1

19 June 04

Analysis of Twente Measurements on Heat Treated RHIC Wire

1.  Introduction

Andries den Ouden has recently measured [1] the magnetization of RHIC wire sample 91-O-80058-A-11 with the same BNL heat treatment as applied to dipole 001.  This note analyses the data for Jc(B) andet(B) to provide input for an updated estimate of Dipole 001 losses in Rep 22.  The resulting et(B) is compared with calculation.  Methods used are exactly the same as Rep 19(2).

2. Data Reduction

Appendix 21-1contains all the data produced by Andries, plus my analysis.  Sheet 'M@B B`' extracts the magnetization at defined B points by selecting points on either side of the defined B and using linear interpolation.   Thus, for each value of B, we find 4 values of M in the 4 quadrants of the M vs B plot.  I then take the mean of these 4 values, which eliminates the reversible magnetization and any slant of the M vs B plot.  The sheet 'sum'ry' plots the mean magnetization against B` (=dB/dt) for each of the defined field points and fits a straight line.  The intercept of this line gives the hysteresis magnetization, from which we calculate Jc(B), and the slope gives the inter-filament coupling, from which we calculate et(B).

3. Calculation of Jc(B) from Magnetization Data

Appendix 21-1 sheet 'Jc(B)' takes the intercepts from the M vs B` plots and uses:

M=23πλfJcdf	(1)

to calculate  Jc(B).  Fig 1 plots the result.  Using the Excel solve routine, I then fit the data to my usual approximation:

Jc=JoBoB+Bo+A0+A1B	(2)

and find the coefficients

Jo = 3.5010 10 A.m-2

B0 = 0.149 T

A0 = 5.0010 9 A.m-2

A1 = -7.0010 8  A.m-2.T -1

These values may be used in calculating losses.

For calculating the transport current enhancement of hysteresis loss, the simple Kim Anderson model (which gives a much worse fit) is shown by the green line in Fig 1 and uses the following coefficients:

J so = 3.2010 10 A.m-2

B so = 0.5 T

Also shown are the transport current Jc measurements on the same wire by Arup Ghosh [2].

Fig 1: Critical current density from magnetization and transport current measurements

4. Calculation of  et(B) from Magnetization Data

The sheet 'Rho(B)' of Appendix 21-1 uses the fitted slopes of the M vs B` plots to calculate et(B).  Recap that, for this calculation we must use the magnetization Mfb defined over the volume enclosed within the filament boundary (of radius afb) calculated from:

Mfb=Maw2afb2 			(3)

Using the relationship:

τ=μo Mfb2B	(4)

the time constant is calculated, and from it the effective transverse resistivity et

ρet=μo2τp2π2 	(5)

so that

ρet=BMfbp2π2

Fig 2 plots this resistivity against field; fitting it with a straight line we have:

et (B)= 1.2410 -10  + 9.010 -11 B   	(6)

with et in m and B in Tesla.   Also shown is the result from Report 19(2)

Fig 2: Measured effective transverse resistivity vs field.

5. Calculation of  et(B) from Copper Resistivity

Sheet 'calculate Rho' of Appendix 19-1 calculates et(B)  in just the same way as Report 19-1, using the measured RRR for this wire of 198.  Fig 3 shows the result, using the two usual approximations of good and poor contact between the NbTi filaments and the copper.  It may be seen that the poor contact approximation gives a fairly good fit.

Fig 3: Calculated effective transverse resistivity compared with measured.

Appendices

Appendix 21-1(1): Analysis of the Twente Magnetization Data

References

[1]  A den Ouden:  Workbook 'BNL-91-0-80058-A-11 V2.xls', dated 17 June 2004, distributed by email

[2]  AK Ghosh 'Superconductor Wire Test # 2111, 7/12/2002', supplied by email 18 Jun 2004