## GSI Fast-Pulsed Synchrotron Magnet Project: MNW Report GSI 3 version 2

## Martin Wilson 30 Dec  00

AC Losses for Different Cycles in RHIC Dipole Magnets

###### Preface

An error has been found in the field components which are the basis of all ac loss calculations in Reports 1 to 4.  The error occurred in converting from Cartesian to polar  components of field and had the effect of increasing the transverse or ‘’ component of field, particularly near to the poles, thereby increasing the total loss by about a factor 2.  Please destroy Report 3-1

##### Introduction

This report adds to Report 2 by calculating the losses for two additional cables based on the measured coupling time constant for the Furukawa wire with copper nickel barriers (Kaugerts J, Jungst K-P et al, IEEE Trans. Appl Superconductivity Volume 10 No 1 pp 824).  Cable ‘core 3’ uses the Furukawa wire as it is, core 4 uses a similar wire with smaller filaments.   Everything else is as described in Report 2-1

# Table 2: Key parameters of cables used in the ac loss calculations

| parameter |  | RHIC | core 1 | core 2 | core 3 | core 4 | unit |
| --- | --- | --- | --- | --- | --- | --- | --- |
| cable half width | a | 4.87E-03 | 4.87E-03 | 4.87E-03 | 4.87E-03 | 4.87E-03 | m |
| cable half thickness | b | 5.83E-04 | 5.83E-04 | 5.83E-04 | 5.83E-04 | 5.83E-04 | m |
| cable twist pitch | p | 7.40E-02 | 7.40E-02 | 7.40E-02 | 7.40E-02 | 7.40E-02 | m |
| crossover resistance | Rc | 5.00E-05 | 1.00E-03 | 4.00E-03 | 4.00E-03 | 4.00E-03 | m |
| adjacent resistance | Ra | 3.50E-04 | 2.00E-05 | 9.00E-05 | 9.00E-05 | 9.00E-05 | W |
| number of strands | N | 30 | 30 | 30 | 30 | 30 |  |
| crossover resistance. area | rc | 4.00E-11 | 8.00E-10 | 3.20E-09 | 3.20E-09 | 3.20E-09 | m2 |
| adjacent resistance. area | ra | 2.80E-10 | 1.60E-11 | 7.20E-11 | 7.20E-11 | 7.20E-11 | m2 |
| effective longitudinal resistivity | x | 2.89E-08 | 1.65E-09 | 7.42E-09 | 7.42E-09 | 7.42E-09 | m |
| cable filling factor | c | 0.826 | 0.826 | 0.826 | 0.826 | 0.826 |  |
| wire filling factor | w | 0.872 | 0.872 | 0.872 | 0.872 | 0.872 |  |
| filament filling factor | f | 0.308 | 0.308 | 0.308 | 0.308 | 0.308 |  |
| wire transverse resistivity | t | 5.67E-10 | 5.67E-10 | 5.67E-10 | 6.13E-09 | 6.13E-09 | m |
| wire twist pitch | pw | 1.33E-02 | 6.00E-03 | 4.00E-03 | 5.30E-03 | 5.30E-03 | m |
| wire coupling time const |  | 4.99E-03 | 1.01E-03 | 4.49E-04 | 7.30E-05 | 7.30E-05 | s |
| filament diameter | df | 6.00E-06 | 6.00E-06 | 6.00E-06 | 6.00E-06 | 2.00E-06 | m |

Table 3: Results of the loss calculations

| cycle # | cable type  | RHIC | core 1 | core2 | core 3 | core 4 |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | ramping total loss / magnet = | 956 W | 171 W | 93 W | 77W | 39W |
| 1 | time averaged total loss / magnet = | 956 W | 171 W | 93 W | 77W | 39W |
| 1 | transverse crossover loss / total = | 71.8% | 20.0% | 9.2% | 11.1% | 22.1% |
| 1 | transverse adjacent loss / total = | 0.21% | 20.7% | 8.5% | 10.2% | 20.2% |
| 1 | parallel loss / total = | 0.01% | 0.69% | 0.28% | 0.34% | 0.68% |
| 1 | filament coupling loss / total = | 22.0% | 25.0% | 20.4% | 4.0% | 7.9% |
| 1 | hysteresis loss / total = | 6.0% | 33.6% | 61.6% | 74.3% | 49.1% |
| 2 | ramping total loss / magnet = | 943 W | 157 W | 79 W | 63W | 34W |
| 2 | time averaged total loss / magnet = | 353 W | 59 W | 30 W | 24W | 13W |
| 2 | transverse crossover loss / total = | 72.8% | 21.8% | 10.8% | 13.5% | 25.0% |
| 2 | transverse adjacent loss / total = | 0.21% | 22.5% | 9.9% | 12.4% | 22.9% |
| 2 | parallel loss / total = | 0.01% | 0.75% | 0.33% | 0.42% | 0.77% |
| 2 | filament coupling loss / total = | 22.3% | 27.1% | 23.9% | 4.9% | 9.0% |
| 2 | hysteresis loss / total = | 4.6% | 27.7% | 55.0% | 68.8% | 42.3% |
| 3 | ramping total loss / magnet = | 187 W | 37 W | 22 W | 19W | 8.9W |
| 3 | time averaged total loss / magnet = | 113 W | 22 W | 13 W | 11W | 5.3W |
| 3 | transverse crossover loss / total = | 70.1% | 17.8% | 7.5% | 8.6% | 18.5% |
| 3 | transverse adjacent loss / total = | 0.21% | 18.4% | 6.8% | 7.9% | 17.0% |
| 3 | parallel loss / total = | 0.01% | 0.61% | 0.23% | 0.26% | 0.57% |
| 3 | filament coupling loss / total = | 21.5% | 22.1% | 16.5% | 3.1% | 6.7% |
| 3 | hysteresis loss / total = | 8.1% | 41.2% | 69.0% | 80.1% | 57.3% |